## Slide 1
A world leader in the development of high performance piezoelectric single crystals MEMS applications.
22, Gaetbeol-ro 145Beon-gil,
Yeonsu-gu, Incheon(21999), Korea
Tel : 82-32-851-2908/2953
Fax : 82-32-851-2907
E-mail : sanggoo7@ibule.com
soisoi77@ibule.com
MEMS APPLICATIONS
SC MEMS
드론/레이저 무기제어용
MEMS Mirror 구동기

## Slide 2
    SC MEMS, Inc. has process that can bond PMN-PT Single Crystal on silicone wafer and process it into thickness appropriate to application. Application is possible in products such as MEMS acoustic sensor or P-MUT (Piezoelectric micromachined ultrasonic transducers).
Film Piezo single crystal(FPSC) MEMS Applications
    FPSC MEMS deformable mirror
    FPSC Energy Harvest : Nano-generator
    FPSC MEMS resonator
    FPSC MEMS accelerometer
    Flexible Single Crystalline PMN-PT Piezoelectric Energy Harvester
    Bending : Generation of high current signal of up to 0.223 mA and output voltage of 8.2 V
A
A
PMN-PT single crystal
Size : normal 20 * 20, max 40 * 40
Thickness : minimum about 5um
Electrode(option) : anything possible
epoxy
Si or SOI wafer
Electrode(option) : anything possible
 | PZT | PMN-PT
Voltage sensitivity (mV/g) | 0.31 | 0.75
Charge sensitivity (pC/g) | 0.026 | 0.4
Resonance Freq. (kHz) | 11 | 10
Size (mm) | 10 x 10 | 10 x 11
Single crystal PMN-PT block bonded on an SOI wafer (thickness 30um)
19 annular ring type actuators
17 mm diameter membrane
Large stroke over 10 um at 20 V for each actuator
High operating bandwidth up to 874 Hz
Items | Specification
PMN-PT | Thickness : 8um
Mother substrate | Silicon wafer
Stressor | Ni film (Thickness : 20um)
Plastic substrate | Polyethylene terephthalate(PET)
Actuator side
Mirror side
More controlled temperature dependence
No need for a stable driving source
Better long term stability
Higher possible band width
The advantages of the use of piezoelectric.
Ref. Journal of Microelectromechanical Systems, Volume: 20 , Issue: 6 , Dec. 2011
Ref. Advanced Materials, Volume 26, Issue 28, July 23, 2014
    0.8~1.5GHz resonance using [001] single crystal
    Wine-Glass mode resonators using [011] single crystal
    Wideband resonator

## Slide 3
    SC MEMS had successfully developed the Lidar sensor using Piezo Single Crystal PMN-PT actuator, and fabrication processing sizes up to 8 inch diameter.
Film Piezo single crystal(FPSC) MEMS Lidar
638nm
Laser Diode
PMN-PT 1
PMN-PT 2
Function
Generator
PMN-PT
1D MEMS Scanner
Out-of-phase
actuation
VIN : IN1, G2
Ground : G1, IN2
Optical scan angle of 30°
Resonance Frequency [kHz] | 30° Drive Voltage [Vpp]
3.5 | 5.5
No. 1
No. 2
No. 3
No. 4
No. 5
No. 6

## Slide 4
Single Crystal Properties
Parameter | Units | [001] poled |  | [011] poled | 
 |  | Low-PT | High-PT | Low-PT | High-PT
ε33T/εo | - | 4842 | 7000 | 3760 | 5770
dij | x 10-12 C/N | d33=1282 | d33=1620 | d32=-1140 | d32=-1820
sijE | x 10-12 m2/N | s33E=47 | s33E=56 | s22E=53 | s22E=78
Trt | oC | 95 | 85 | 95 | 85
Ec | KV/cm | 2 | 2.5 | 2 | 2.5
Density | Kg/m3 | 8080 |  |  | 
PMN-PT
PIN-PMN-PT
Unique piezocrystal properties create opportunities for unprecedented system performance.
Parameter | Units | [001] Poled |  | [011] Poled | 
 |  | Low-PT | High-PT | Low-PT | High-PT
ε33T/εo | - | 4457 | 5666 | 3449 | 4656
dij | x 10-12 C/N | d33=1226 | d33=1840 | d32=-1323 | d32=-1870
sijE | x 10-12 m2/N | s33E=49 | s33E=79 | s22E=72 | s22E=99
Trt | oC | 120 | 90 | 120 | 90
Ec | KV/cm | 4 | 6 | 4 | 6
Density | kg/m3 | 8154 |  |  |